## Slide 1: Bangladesh University Of Textiles
Project Title:
A Sustainable Approach: A Scope of Using the Solid Textile Cotton Wastage in Hygiene Product (Sanitary Pad) Manufacturing

## Slide 2: This project is
Supervised By,
      Md. Abdullah Al. Mamun
      Assistant Professor,
      Dept. of Fabric Engineering
Presented By,
        Md. Shihab Alam
        2016-1-2-019
        Md. Saiful Islam
        2016-1-2-050
        Tanmoy Mitra
        2016-1-2-051

## Slide 3
Bangladesh 8%
Vietnam 5%
Italy 5%
Germany 4%
Textile Industries | Unit in number
Spinning | 425
weaving | 400
Knitting | 2500
Garment | 4621
TEXTILE CONTRIBUTION
351,000 tons wastes annually

## Slide 4: Uses of recycled textile wastages
PCW Yarn
Insulation Cloth
Wicking Cloth
Paper
Decorative Product

## Slide 5: Scope
All the materials used for manufacturing of sanitary are imported. If any of the material can be replaced by textile wastage, it will be a huge contribution for sanitary napkin industry and the price also can be minimized.
Replacement of fluff Pulp of absorbent layer by cotton is the main focus of this project.

## Slide 6: Market Scenario
Some available pads in market
Market share and growth

## Slide 7: Objectives
The objectives of our project are:
        To produce sanitary napkin from Textile cotton wastage
        To produce sanitary pad at a affordable price
        To reduce the environmental pollution

## Slide 8: Raw Materials
Wastages from different section are used as raw material:-
Spinning Industry Wastage
Knitting Industry Wastage
Weaving Industry Wastage
Garment Industry Wastage

## Slide 9: Recycling Process of Wastage
Cutting
Tearing
Opening & Cleaning

## Slide 10: Processing of raw materials
Bleaching/Stripping
Trash analyzing
Carding

## Slide 11: Different forms of Raw materials
Wastages
Fiber
Carded Lap

## Slide 12: Production process
There is 5 steps of sanitary napkin production;
            Crashing
            Compressing
            Wrapping
            Sterilizing
            Packaging

## Slide 13: Produced Sample
Parameters | Value(average)
Length | 198 mm
Width | 68 mm
Thickness | 14 mm
Weight | 15 gm
Dimension of produced sample:

## Slide 14: Different types of tests
The following Tests are carried out:
      Absorption Capacity Test
      PH Test
      Ability To withstand Pressure After Absorption
      Penetration Test
      Antimicrobial Test

## Slide 15: Absorption capacity test
The Sample was immersed into demineralised water for 30 min.
The sample hang vertically in a stand for 30 min to release the extra water by gravity.

## Slide 16: Absorption Test result
Chart: Absorption Test
| Sample 1 | Sample 2 | Sample 3 | Sample 4
absorption test | 112 | 110 | 115 | 110
The standard range of absorption is 95-105 mL

## Slide 17: Ph test
0.5 gm sample was cut from core of the pad
and mixed with 100 ml demineralised Water for 1 hour.
After 1 hour the PH was measured by PH meter.

## Slide 18: PH Test result
Chart: PH Test
| sample 1 | sample 2 | sample 3 | sample 4
PH Value | 7.1 | 6.9 | 7.33 | 6.8
The standard range of PH is 5.5-8.5

## Slide 19: Ability To withstand Pressure After Absorption
30 ml K2Cr2O7 (1% solution) was
poured on the sample.
Then 1 kg load was applied on the sample
for 1 minute.

## Slide 20: Ability To withstand Pressure After Absorption result
Liquid retention was comparatively low which causes side leakage

## Slide 21: Penetration test
Liquid Strike through Time Tester
20 ml of 1% saline solution poured on the sample
with 3 ml/sec releasing speed.

## Slide 22: Penetration Test result
Chart: 
| sample 1 | sample 2 | sample 3 | sample 4
Penetration Time | 4.5 | 4.93 | 4.76 | 4.58
The standard range of Penetration Time is 2-2.5 sec

## Slide 23: Hydro gel Distribution
Top layer
Bottom layer

## Slide 24: Cost Analysis
Cost of producing sanitary pad from recycled cotton
Materials & Factory Overhead | Price | Cost of making one pad
Textile Cotton Wastage | BDT 46/kg | BDT 0.46
PE sheet (bottom layer) | USD 2.96/kg BDT 250/kg | USD 0.0041 BDT 0.35
Non-woven (top layer) | USD 3.13/kg BDT 265/kg | USD 0.0044 BDT 0.37
Factory Overhead |  | BDT 1
 |  | Total = 2.16 BDT
Chart: 
| Joya | Senora | Freedom | Anannya | Pad Produced by Cotton wastage
Cost of Different Pads | 7.5 | 13.75 | 12.5 | 5 | 2.16

## Slide 25: Future Prospects
To attain more liquid retention fluff pulp will be mixed at different proportion to optimized the quality.
To get better performance and comfortability hydrogel arrangement will be improvised.
The non-biodegradable nonwoven outer and inner layer and the polyethylene back sheet will be replaced by biodegradable materials.
As diaper has the same requirement textile waste will also use in it.

## Slide 26
THANKS
For Being With Us